## Slide 1: Fast Search for Perovskite Materials with Improved Solubility
Henry Herbol, Weici Hu, and Matthias Poloczek SEED Meeting, Oct 18 2016
Notes: Henry Herbol, Weici Hu, and Matthias Poloczek

## Slide 2: Motivation, Setup, and Goal
The Motivation: Lead halides are poorly solvable. “Undissolved parts will not only be wasted in the reaction, but also interfere with the homogeneity of the resulting films.” (Stevenson et al.’16) Improve the solubility of lead halides (c Pbn+ h3 ) The Setup: Given a Cation c, a Halide Ion h, and a Solvent s, we can estimate the solubility of the perovskite material in s. The estimation is performed via molecular dynamics (MD) and density functional theoretical (DFT) computations (-> Henry).
The Goal: Choose
c among Methylammonium (MA), Formamidinium (FA), or Cesium (Cs),
h among Cl, Br, and I, and
one out of 15 solvents,
in order to maximize the solubility (enthalpy of solution or Mayer Bond order). Thus, we optimize over 135 candidates. Evaluating one candidate takes about 1 week of CPU time (single core).
Notes:   lead bromide, lead iodide, and lead chloride

## Slide 3: Bayesian Optimization for Experimental Design
Our approach relies on two components:
A Bayesian statistical model that predicts a solubility for each combination, based on previously collected data. We suppose a linear model, where the halide ion, cation, and solvent contribute linearly to the solubility (-> Weici). Similar combinations will have “similar” solubilities.
An acquisition function that selects the experiment to conduct next, based on a value of information analysis that prioritizes the most promising combination. We always select a combination whose expected improvement over the current best solubility is maximum.

## Slide 4: Bayesian Statistical Model
Let ax denote the contribution of each halide ion and cation, e.g. x = Cl or MA. We will estimate ax from data. Let 1x be one if the halide/cation is present in the compound and zero otherwise.
Let gamma_s denote the contribution of the solvent.
The solubility of combination z is given by Sol_z = aCl 1CL + aBr 1Br + … + aCs 1Cs + gamma_s + beta_z.

## Slide 5: Expected Improvement Acquisition Function
Notes: Observations are noiseless, therefore EI should be good